## Slide 1: Annual Review
Studies of VO2 Thin Films with Ultrafast pulses and Raman spectroscopy.
Elizabeth Radue
3/11/12

## Slide 2: Course Requirements
Entered program in 2010
Completed all core class requirements
Electives
  Out of Field: completed
  In Field: in process
Completed Qualifying Exam: Summer 2011

## Slide 3: Research
Working in Irina Novikova’s Lab, (closely with Lukaszew)
Collaboration working on VO2 thin films
Notes: Summer 20011

## Slide 4: VO2 Insulator Metal Transition
VO2 transition from insulator to metal when heated or optically stimulated

## Slide 5: Ultrafast Laser system
100fs pulse with repetition rate of 1kHz
800nm: optional wavelengths from 400nm-1600nm

## Slide 6: Pump-probe Experimental Set up
Legend Elite 800nm
Variable Delay
Lock-in Amplifier
Computer
Detector
Variable ND filter
sample

## Slide 7
Observe transition by observing change in reflectivity

## Slide 8: Intensity of Probe beam

## Slide 9: Why mount films in a cryostat?
Effects of Temperature vs. Strong electric fields freeing electrons
 Some controversy as to the main cause: fast response suggests electronic response vs. change in crystal lattice
T. Cocker, L. Titova, S. Fourmaux, G. Holloway, H.-C. Bandulet, D. Brassard, J.-C. Kieffer, M. El Khakani, and F. Hegmann, Physical Review B 85, 155120 (2012).
D. Hilton, R. Prasankumar, S. Fourmaux, a. Cavalleri, D. Brassard, M. El Khakani, J. Kieffer, a. Taylor, and R. Averitt, Physical Review Letters 99, 226401 (2007).

## Slide 10: Varying temperature in Cryostat

## Slide 11: Different Substrates
Different Recovery Responses

## Slide 12: Anisotropy w/ TiO2

## Slide 13: Raman Spectroscopy
Collaboration with Buzz Wincheski at NASA Langley
Backscattering configuration
Tried different wavelengths for incident beam
Compared films on different substrates

## Slide 14: Different wavelengths
VO2 on quartz
VO2 on sapphire

## Slide 15
VO2 film on sapphire
VO2 on quartz
Raman Spectra through IMT

## Slide 16
VO2 on TiO2

## Slide 17: Peak 224cm-1 fit
VO2 film on quartz
VO2film on sapphire

## Slide 18: Change in background levels in peak fitting
VO2 film on quartz
VO2film on sapphire

## Slide 19: Plans for the Future
Immediate:
  New XRD allows for growth of new films
  Writing up results for Raman spectroscopy
  Build autocorrelator for beam characterization
Down the Road:
  Use pump probe to study dynamics of surface plasmon polaritons
  Graduate 2016

## Slide 20: Transmitted vs. Reflected Beam

## Slide 21: XRD
VO2 on Quartz
VO2 on Sapphire
VO2 on TiO2

## Slide 22: Multiple peak fits on VO2 on SiO2

## Slide 23: Polarization of incident/reflected beam